REPORT ON MIX DESIGN OF DENSE BITUMINOUS MACADAM GRADE II

Phase3 Binder Test

Pavement Laboratory  •  Report Date: 14-May-2026

Project Information

| Item | Detail |
| --- | --- |
| Name of Work | Phase3 Binder Test |
| Binder Grade | CRMB |

Binder Properties

| Property | Value |
| --- | --- |
| Specific Gravity | 1.025 |
| Penetration @25°C (1/10 mm) | 65 |
| Softening Point (°C) | 55 |

Notes: Sample 21-A

1. Materials

2. Aggregate Gradation (% Passing)

| IS Sieve (mm) | 25mm | 20mm | 6mm | SD | Cement |
| --- | --- | --- | --- | --- | --- |
| 37.5 | 100.0 | 100.0 | 100.0 | 100.0 | 100.0 |
| 26.5 | 96.6 | 100.0 | 100.0 | 100.0 | 100.0 |
| 19 | 44.5 | 89.8 | 100.0 | 100.0 | 100.0 |
| 13.2 | 4.0 | 5.2 | 100.0 | 100.0 | 100.0 |
| 4.75 | 0.0 | 0.0 | 38.6 | 99.8 | 100.0 |
| 2.36 | 0.0 | 0.0 | 8.1 | 92.3 | 100.0 |
| 0.3 | 0.0 | 0.0 | 0.0 | 33.8 | 100.0 |
| 0.075 | 0.0 | 0.0 | 0.0 | 9.5 | 42.2 |

3. Blend Proportions

| Aggregate | Proportion |
| --- | --- |
| 25mm | 23.0% |
| 20mm | 11.0% |
| 6mm | 32.0% |
| SD | 32.0% |
| TOTAL | 98.0% |

Aggregates are mixed in the proportions above to meet the combined gradation specified for Dense Bituminous Macadam Grade II (MoRTH).

4. Combined Gradation vs Specification

| IS Sieve (mm) | Combined % Passing | MoRTH Spec | Status |
| --- | --- | --- | --- |
| 37.5 | 98.00 | 100 – 100 | Out |
| 26.5 | 97.21 | 90 – 100 | Within |
| 19 | 84.12 | 71 – 95 | Within |
| 13.2 | 65.49 | 56 – 80 | Within |
| 4.75 | 44.27 | 38 – 54 | Within |
| 2.36 | 32.11 | 28 – 42 | Within |
| 0.3 | 10.81 | 7 – 21 | Within |
| 0.075 | 3.03 | 2 – 8 | Within |

5. Specific Gravities of Materials

| Material | Bulk Sp. Gr. | Water Absorption |
| --- | --- | --- |
| Coarse 25mm | 2.718 | 2.51% |
| Coarse 20mm | 2.695 | 3.02% |
| Fine 6mm | 2.803 | — |
| Fine SD | 2.758 | — |
| Bitumen (CRMB) | 1.011 | — |
| Combined aggregate (Gsb) | 2.756 | — |

6. Marshall Mix Design Summary

| Pb % | Gmm | Gmb | VIM % | VMA % | VFB % | Stab. kN | Flow mm | MQ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3.5 | 2.589 | 2.443 | 5.66 | 14.45 | 60.84 | 12.22 | 3.36 | 3.64 |
| 4.0 | 2.569 | 2.452 | 4.54 | 14.58 | 68.86 | 14.03 | 3.44 | 4.08 |
| 4.5 | 2.548 | 2.460 | 3.48 | 14.76 | 76.43 | 16.26 | 3.62 | 4.49 |
| 5.0 | 2.528 | 2.446 | 3.23 | 15.66 | 79.38 | 14.43 | 3.76 | 3.84 |
| 5.5 | 2.508 | 2.436 | 2.89 | 16.47 | 82.44 | 13.59 | 3.88 | 3.50 |

7. Optimum Bitumen Content (OBC)

OBC = 4.25% (at target 4.0% air voids — method: interpolated)

Mix Parameters at OBC vs Specification

| Property | Value at OBC | Requirement | Status |
| --- | --- | --- | --- |
| Stability (kN) | 15.16 | ≥ 9.0 | PASS |
| Flow (mm) | 3.53 | 2.0 – 4.0 | PASS |
| Air Voids (%) | 4.00 | 3.0 – 5.0 | PASS |
| VMA (%) | 14.67 | ≥ 13.25 | PASS |
| VFB (%) | 72.71 | 65.0 – 75.0 | PASS |
| Marshall Quotient | 4.30 | 2.0 – 5.0 | PASS |
| Gmb at OBC | 2.456 | — | — |
| Gmm at OBC | 2.558 | — | — |

Overall compliance (Dense Bituminous Macadam Grade II): PASS

8. Material Calculation for Sample Preparation

Quantities to weigh out when preparing a Marshall specimen of the standard sample (left bitumen content) and the target preparation sample (right bitumen content), with dry-material breakdown by aggregate fraction.

| Block | Pb % | Aggregate % | Aggregate wt (g) | Bitumen wt (g) | Total mix wt (g) |
| --- | --- | --- | --- | --- | --- |
| Standard sample | 4.50 | 95.50 | 1200.00 | 56.54 | 1256.54 |
| Target sample | 4.00 | 96.00 | 1206.28 | 50.26 | 1256.54 |

Dry Material — Standard Sample

| Particle Size | Blend Ratio | Weight (g) |
| --- | --- | --- |
| 25mm | 23.0% | 276.00 |
| 20mm | 11.0% | 132.00 |
| 6mm | 32.0% | 384.00 |
| SD | 32.0% | 384.00 |
| Cement | 2.0% | 24.00 |
| TOTAL | 100.0% | 1200.00 |

Dry Material — Target Sample

| Particle Size | Blend Ratio | Weight (g) |
| --- | --- | --- |
| 25mm | 23.0% | 277.45 |
| 20mm | 11.0% | 132.69 |
| 6mm | 32.0% | 386.01 |
| SD | 32.0% | 386.01 |
| Cement | 2.0% | 24.13 |
| TOTAL | 100.0% | 1206.28 |

9. Marshall Design Curves

| Prepared By ______________________ | Approved By ______________________ |
| --- | --- |